# TEST REPORT

Report No.:AZT251219005C-E0                               Date of issue: December 24, 2025                 Page 1 of 10

| Applicant | : | Yueqing Yongdong Electric Motor Technology Co., Ltd. |
| --- | --- | --- |
| Address | : | No. 307, 19th Weilu Road, Yueqing Economic Development Zone, Yueqing City, Wenzhou City, Zhejiang Province, P.R. China |
| Manufacturer | : | Yueqing Yongdong Electric Motor Technology Co., Ltd. |
| Address | : | No. 307, 19th Weilu Road, Yueqing Economic Development Zone, Yueqing City, Wenzhou City, Zhejiang Province, P.R. China |

Report on the submitted samples said to be:

| Sample Name | : | Motor coil |
| --- | --- | --- |
| Model No. | : | YD6W-8KW/Single (Three)-Phase Asynchronous Motor Coil, Model: YD6W-8KW |
| Date of Sample Received | : | December 19, 2025 |
| Testing Period | : | December 19, 2025 ~ December 24, 2025 |
| Results | : | Please refer to next page(s). |

******************************************************************************************************************************

TEST REQUEST                                                                                                 CONCLUSION

According to the customer's request, based on the performed tests on submitted sample, the result of Lead, Cadmium, Mercury, Hexavalent Chromium, PBBs, PBDEs, Dibutyl

Pass

Phthalate (DBP), Benzyl butyl Phthalate (BBP), Bis(2-ethylhexyl) Phthalate (DEHP), Diisobutyl phthalate (DIBP) content comply with the limit as set of RoHS Directive   2011/65/EU Annex II amending Directive (EU)2015/863.

******************************************************************************************************************************

Signed for and on behalf of AZT

Jack Zhong

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com

TEST REPORT

Report No.:AZT251219005C-E0                              Date of issue: December 24, 2025                 Page 2 of 10

Test Item Description And Photo List

| No. | Tested Part(s) | The photo of the sample |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 01 | Red tape | 04 |  |  |  |  |  |
| 02 | White textile with transparent glue |  |  |  |  |  |  |
| 03 | Copper metal coil | 01 | 02. 03. | 05 06 |  | '\ 08-09 07. |
| 04 | Light blue plastic |  |  |  |  |  |  |
| 05 | Silvery metal |  |  |  |  |  |  |
| 06 | Blue wire jacket |  |  |  |  |  |  |
| 07 | Red wire jacket |  |  |  |  |  |  |
| 08 | Yellow wire jacket |  |  |  |  |  |  |
| 09 | Silvery metal core |  |  |  |  |  |  |
| 10 | Black soft plastic | 10 | 11 | 12 |  | 13 |  |
| 11 | Silvery metal |  |  |  |  |  |  |
| 12 | Silvery metal |  |  |  |  |  |  |
| 13 | Silvery metal with rose golden plating |  |  |  |  |  |  |

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com

# TEST REPORT

Report No.:AZT251219005C-E0                              Date of issue: December 24, 2025                 Page 3 of 10

Results:

RoHS Directive 2011/65/EU Annex II amending Directive (EU)2015/863

A. XRF screening Result

Test method: With reference to IEC 62321-3-1:2013, Screening by X-ray Fluorescence Spectroscopy (XRF)

| No. | Tested Part(s) | Results |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Cd | Pb | Hg | Cr▽ | Br▽ |  |
|  |  |  |  |  |  | PBBs | PBDEs |
| 01 | Red tape | BL | BL | BL | BL | BL | BL |
| 02 | White textile with transparent glue | BL | BL | BL | BL | BL | BL |
| 03 | Copper metal coil | BL | BL | BL | BL | / | / |
| 04 | Light blue plastic | BL | BL | BL | BL | BL | BL |
| 05 | Silvery metal | BL | BL | BL | BL | / | / |
| 06 | Blue wire jacket | BL | BL | BL | BL | BL | BL |
| 07 | Red wire jacket | BL | BL | BL | BL | BL | BL |
| 08 | Yellow wire jacket | BL | BL | BL | BL | BL | BL |
| 09 | Silvery metal core | BL | BL | BL | BL | / | / |
| 10 | Black soft plastic | BL | BL | BL | BL | BL | BL |
| 11 | Silvery metal | BL | BL | BL | BL | / | / |
| 12 | Silvery metal | BL | BL | BL | BL | / | / |
| 13 | Silvery metal with rose golden plating | BL | BL | BL | BL | / | / |

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com

# TEST REPORT

Report No.:AZT251219005C-E0                              Date of issue: December 24, 2025                 Page 4 of 10

Note:

( 1)      Results were obtained by XRF for primary screening, and further chemical testing by ICP (for Cd, Pb, Hg) , UV-Vis (for Cr(Ⅵ)) and GC-MS (for PBBs , PBDEs) are recommended to be performed, if the

concentration exceeds the below warning value according to IEC 62321-3-1:2013.

XRF screening limits for different materials:

| Element | Unit | Non-metal | Metal | Composite Material |
| --- | --- | --- | --- | --- |
| Cd | mg/kg | BL≤70-3σ<X <130+3σ≤OL | BL≤70-3σ<X <130+3σ≤OL | BL≤50-3σ<X <150+3σ≤OL |
| Pb | mg/kg | BL≤700-3σ<X <1300+3σ≤OL | BL≤700-3σ<X <1300+3σ≤OL | BL≤500-3σ<X <1500+3σ≤OL |
| Hg | mg/kg | BL≤700-3σ<X <1300+3σ≤OL | BL≤700-3σ<X <1300+3σ≤OL | BL≤500-3σ<X <1500+3σ≤OL |
| Cr | mg/kg | BL≤700-3σ<X | BL≤700-3σ<X | BL≤500-3σ<X |
| Br | mg/kg | BL≤300-3σ<X | -- | BL≤250-3σ<X |

Note:

-        BL=Below Limit

-        OL=Over Limit (Screening result was over limit , thus further confirmation test was conducted.)

-        X= Inconclusive(Screening result was inconclusive, thus further confirmation test was conducted.)

-        /= Not Applicable

-        mg/kg = milligram per kilogram = ppm

(2)     The XRF screening test for RoHS elements – The reading may be different to the actual content in the sample be of non-uniformity composition.

(3)     The maximum permissible limit is quoted from the RoHS Directive 2011/65/EU Annex II amending Directive (EU)2015/863.

(4)     ▽=For restricted substances PBBs and PBDEs, the results show the total Br content; The restricted substance was Cr (Ⅵ), and the results showed the total Cr content.

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com

# TEST REPORT

Report No.:AZT251219005C-E0                              Date of issue: December 24, 2025                 Page 5 of 10

| RoHS Restricted Substances | Maximum Concentration Value (mg/kg) (by weight in homogenous materials) |
| --- | --- |
| Cadmium (Cd) | 100 |
| Lead (Pb) | 1000 |
| Mercury (Hg) | 1000 |
| Hexavalent Chromium (Cr(Ⅵ)) | 1000 |
| Polybrominated biphenyls (PBBs) | 1000 |
| Polybrominated diphenyl ethers (PBDEs) | 1000 |
| Dibutyl Phthalate (DBP) | 1000 |
| Benzyl butyl Phthalate (BBP) | 1000 |
| Bis(2-ethylhexyl) Phthalate (DEHP) | 1000 |
| Diisobutyl phthalate (DIBP) | 1000 |

Disclaimers:

This XRF Screening report is for reference purposes only. The applicant shall make its/his/her own judgment as to whether the information provided in this XRF screening report is sufficient for its/his/her purposes.

The result shown in this XRF screening report will differ based on various factors, including but not limited to, the sample size, thickness, area, surface flatness, equipment parameters and matrix effect (e.g. plastic, rubber, metal, glass, ceramic etc.). Further wet chemical pre-treatment with relevant chemical equipment analysis are   required to obtain quantitative data.

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com

# TEST REPORT

Report No.:AZT251219005C-E0                              Date of issue: December 24, 2025                 Page 6 of 10

## B. Result of Wet Chemical Testing

Test method:

Lead & Cadmium Content:

With reference to IEC 62321-5:2013, analysis was performed by Inductively Coupled Plasma-Optical Emission Spectrometer (ICP-OES).

Mercury Content:

With reference to IEC 62321-4:2013+AMD1:2017 CSV, analysis was performed by Inductively Coupled Plasma-Optical Emission Spectrometer (ICP-OES).

Hexavalent Chromium Content:

With reference to IEC 62321-7-1:2015& IEC 62321-7-2:2017, analysis was performed by UV-visible spectrophotometer (UV-Vis).

PBBs & PBDEs Content:

With reference to IEC 62321-6:2015, analysis was performed by gas chromatographic-mass spectrometer (GC-MS).

DBP, BBP, DEHP, DIBP Content:

With reference to IEC 62321-8:2017, analysis was performed by gas chromatographic-mass spectrometer (GC-MS).

1) The test results of DBP, BBP, DEHP & DIBP

| Test Items | CAS No. | Unit | MDL | Results |  | Limit |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | 04 | 06+07+08 |  |
| Dibutyl Phthalate (DBP) | 84-74-2 | mg/kg | 50 | N.D. | N.D. | 1000 |
| Benzyl butyl Phthalate (BBP) | 85-68-7 | mg/kg | 50 | N.D. | N.D. | 1000 |
| Bis(2-ethylhexyl) Phthalate (DEHP) | 117-81-7 | mg/kg | 50 | N.D. | N.D. | 1000 |
| Diisobutyl phthalate (DIBP) | 84-69-5 | mg/kg | 50 | N.D. | N.D. | 1000 |

| Test Items | CAS No. | Unit | MDL | Results | Limit |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | 10 |  |
| Dibutyl Phthalate (DBP) | 84-74-2 | mg/kg | 50 | N.D. | 1000 |
| Benzyl butyl Phthalate (BBP) | 85-68-7 | mg/kg | 50 | N.D. | 1000 |
| Bis(2-ethylhexyl) Phthalate (DEHP) | 117-81-7 | mg/kg | 50 | N.D. | 1000 |
| Diisobutyl phthalate (DIBP) | 84-69-5 | mg/kg | 50 | N.D. | 1000 |

Remark:

-    mg/kg = milligram per kilogram = ppm

-    N.D. = Not detected

-    MDL= Method detected limited

-    The samples were mixed for phthalic acid test

-    Tested part(s) was/were specified by client

-    Flow chart appendix is included

-    Photo appendix is included

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com

# TEST REPORT

Report No.:AZT251219005C-E0                               Date of issue: December 24, 2025                 Page 7 of 10

# Appendix

Pb/Cd/Hg/Cr6+ Testing Flow Chart

Sample Preparation

Sample Measurement

Cr6+

Hg

Acid digestion with microwave/ hotplate

Pb/Cd

Metallic material

Nonmetallic material

Acid digestion with microwave/ hotplate

Filtration

Boiling water

Adding digestion

Filtration

Solution

1)Soluble polymer:

Adding 1, 5

adding NMP ultrasound

-diphenylcarbazide

for color

development

Solution                     Residue

1)    Alkali Fusion/Dry Ashing

2)   Acid to dissolve

2)Insoluble polymer: adding alkaline digestion

ICP analyze

solution + toluene, 150℃ -160℃ closed heating

UV-Vis analyze

Filtration and pH adjustment

DATA

DATA

(Negative/

Positive)

Adding 1, 5

-diphenylcarbazide for color development

ICP/AAS analyze

UV-Vis analyze

DATA

DATA

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com

# TEST REPORT

Report No.:AZT251219005C-E0                              Date of issue: December 24, 2025                 Page 8 of 10

# PBBs/PBDEs Testing Flow Chart

Cutting/ Preparation

Weigh Sample

# Sample solvent extraction

Concentration/ Dilution of Extracted solution

Filtration

GC-MS

DATA

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com

# TEST REPORT

Report No.:AZT251219005C-E0                              Date of issue: December 24, 2025                 Page 9 of 10

# Phthalates Testing Flow Chart

Cutting/ Preparation

Weigh Sample

# Sample solvent extraction

Concentration/ Dilution of Extracted solution

Filtration

GC-MS

DATA

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com

# TEST REPORT

Report No.:AZT251219005C-E0                               Date of issue: December 24, 2025               Page 10 of 10

# The photo of the sample

AZT authenticate the photo on original report only

Statement:

1. This test report is invalid without the signature of the approver and the special seal of the company's report.

2. The copy of the test report is invalid if the "Special Seal for Inspection and Testing" or "Special Seal for testing" or the official seal of the testing unit is not re-stamped.

3. After the test report is altered, the test report is invalid.

4. If there is any objection to the test report, please submit written comments to the laboratory within 15 days from the date of receipt of the report.

5. This test is only responsible for samples provided by customers.

6. This report shall not be reproduced in whole or in part without the written authorization of the Company.

7. The laboratory is not responsible for sampling, all samples are provided by customers.

8. The test results in this test report are only related to the samples provided by the customer.

9. If the report is not stamped with the qualification mark, it is only used for scientific research, teaching, internal quality control and other activities, and does not have a proof role for the society.

*** End of Report ***

Shenzhen AZT Technology Co., Ltd.

No.502, Building 1, Yibaolai Industrial City, Qiaotou Community, Fuhai Street, Bao'an District, Shenzhen, Guangdong, China

Tel: 0755-23501189; E-mail: azt-ep@azt-tech.com; Http: www.azt-tech.com